Table 1.  Plagioclase sample characteristics

| Sample | Locality and source | Composition | Notes |
| --- | --- | --- | --- |
| albite* | Amelia Courthouse, VA | Ab98.2An0.2Or1.6 | Qod () = .92a or 1b (pegmatitic) |
| FSU | unknown purchased from Gems ‘N Rough | Ab94An5Or1 | Transparent green, gemmy. Few very small inclusions visible on 010. |
| FON | Hawk Mine, NC Smithsonian NMNH #R2898 | Ab78An19Or3 | Colorless crystal with schiller, albite twins and unidentified 0.3-0.5 mm inclusions. Qod () = .55 b (pegmatitic) |
| FLN | Tabor Island, Nain, Labrador, Canada purchased from Excalibur Mineral Co. | Ab51An47Or2 | Grey color with distinct albite twinning visible on (001). Ilmenite inclusions. Irridescence on (010) suggests Bøggild intergowth. |
| FLT | Tuléar Province, Madagascar | Ab45An52Or2 | “Peacock blue” color with ilmenite inclusions. Irridescence on (010) suggests Bøggild intergrowth. |
| FBM | Mexico purchased from Gems ‘N Rough | Ab39An59Or2 | Large transparent yellowish crystal |
| FLC | Clear Lake, Utah Smithsonian NMNH #C5869 | Ab36An63Or1 | Transparent yellow, gemmy. |
| FLL | Lakeview, Lake Co., Oregon purchased from Minerals Unlimited | Ab33An65Or1 | Labradorite phenocrysts in basalt. Sharp a and b reflections and diffuse e and c reflectionsc. Qod () a = .56 or .67 |
| FMA | Miyake, Japan purchased from Excalibur Mineral Co | Ab5An95Or0 | Sharp a and b reflections, streaked c reflectionsd,e. Small rutile (?) inclusions. |

*analyzed in a previous study (Hofmeister et al, 2009). Order parameters taken from a Angel et al (1990) and  b Tribaudino et al (2010): Qod () = 1 is completely ordered, 0 is completely disordered; Qod () =  0 is , 1 is .  From single crystal x-ray analysis cWenk, 1980, dCarpenter, 1985 and eFoit and Peacor, 1973.

Table 2.  Fits for plagioclase: 1/D = A + B ( 10-3T + C ( 10-6T2 + E ( 10-10T3

| Sample | D298 | A | B | C | E | T range (K) |
| --- | --- | --- | --- | --- | --- | --- |
| albite010 | 1.689 | 0.1253 (2.306x10-2) | 1.827(6.824x10-5) | -0.6582 (4.381x10-8) |  | 298-1250 |
| albite001* | 1.354 | 0.0288 | 0.2568 | -1.024 |  | 298-1075 |
| albite( | 1.077 | 0.1200 (5.961x10-2) | 3.290(1.970x10-4) | -1.364(1.444x10-7) |  | 298-1075 |
| FSU 010 | 1.270 | 0.3348 (3.092x10-2) | 1.783(8.866x10-5) | -0.7322 (5.660x10-8) |  | 298-1258 |
| FSU 001 | 1.102 | 0.4181 (2.254x10-2) | 1.881(7.289x10-5) | -0.8515 (5.322x10-8) |  | 298-1062 |
| FSU (‡ | 0.933 |  |  |  |  |  |
| FON 010 | 0.919 | 0.3560 (8.400x10-2) | 3.210(3.755x10-4) | -2.284 (3.920x10-7) |  | 298-680 |
|  |  | 1.402 (4.283x10-2) | 0.2067(4.189x10-5) |  |  | 800-1200 |
| FON 001 | 0.979 | 0.2010 (1.079x10-1) | 3.554(4.744x10-4) | -2.4876 (4.909x10-7) |  | 298-680 |
|  |  | 1.199 (5.657x10-2) | 0.4280(5.536x10-5) |  |  | 800-1200 |
| FON ( | 0.868 | -0.0289 (0.2116) | 5.105(9.323x10-4) | -3.661 (9.662x10-7) |  | 298-680 |
|  |  | 1.741 (0.1583) | 0.1547(1.554x10-4) |  |  | 800-1200 |
| FLN 010 | 0.892 | 0.5130 (4.658x10-2) | 2.558(1.908x10-4) | -1.564 (1.799x10-7) |  | 298-800 |
|  |  | 0.8134 (0.7410) | 1.610(1.286x10-3) | -0.6672 (5.534x10-7) |  | 1000-1300 |
| FLN 001 | 0.956 | 0.4481 (6.534x10-2) | 2.488(2.664x10-4) | -1.438 (2.501x10-7) |  | 298-800 |
|  |  | 1.605 (1.001) | 0.4041(1.715x10-3) | -1.575 (7.291x10-7) |  | 1000-1300 |
| FLN ( | 0.797 | 0.5346 (6.137x10-2) | 2.948(2.513x10-4) | -1.659 (2.369x10-7) |  | 298-800 |
|  |  | 0.5948 (1.048) | 2.242(1.830x10-3) | -0.8766 (7.927x10-7) |  | 1000-1300 |
| FLT010‡ | 0.780 |  |  |  |  |  |
| FLT001‡ | 0.882 |  |  |  |  |  |
| FLT(‡ | 0.758 |  |  |  |  |  |
| FBM 010 | 0.794 | 0.7837 (5.067x10-2) | 2.162(2.108x10-4) | -1.883(2.535x10-7) | 5.673(9.190x10-11) | 298-1553 |
| FBM 001 | 0.776 | 0.7650(5.054x10-2) | 2.383 (2.102x10-4) | -2.286(2.528x10-7) | 8.168(9.167x10-11) | 298-1553 |
| FBM ( | 0.632 | 0.9755(9.633x10-2) | 2.800(4.335x10-4) | -2.500(5.747x10-7) | 7.968(2.324x10-10) | 298-1357 |
| FLC010‡ | 0.884 |  |  |  |  |  |
| FLC001‡ | 0.836 |  |  |  |  |  |
| FLL 010 | 0.767 | 1.045(7.393x10-2) | 1.266(1.995x10-4) | -0.5651(1.195x10-7) |  | 298-1350 |
| FLL 001 | 0.751 | 1.183(4.232x10-2) | 0.6782(1.142x10-4) | -0.2246(6.843x10-8) |  | 298-1350 |
| FLL ( | 0.811 | 1.0254(8.256x10-2) | 1.211(2.228x10-4) | -5.641(1.333x10-7) |  | 298-1350 |
| FMA010 | 0.724 | 0.4453(9.421x10-2) | 3.669(3.495x10-4) | -1.845(3.023x10-7) |  | 298-870 |
| FMA001 | 0.755 | -0.4337(0.3942) | 8.380(2.004x10-3) | -8.103(2.473x10-6) |  | 298-550 |
|  |  | -0.1622(0.5009) | 5.811(1.322x10-3) | -3.565(8.432x10-7) |  | 551-1050 |

Errors for coefficients are given in parentheses.  *Errors for fits are not included due to large error in measurement. ‡ FSU(, FLT, and FLC were measured at room temperature, only.